Appendix: Table 1

XRF results1 from the technical examination of objects in this catalogue

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Sample** | **n=2** | **Co** | **Cu** | **Zn** | **Ag** | **Cd** | **Sn** | **Sb** | **Au** | **Pb** | **Bi** | **Total3** |  | **Instrument** |
| 82.DG.17 Coat of arms (burnished lobe) | 4 | 0.00 | 1.3 | 0.0 | 98.4 | 0.01 | 0.01 | 0.03 | 0.02 | 0.3 | 0.02 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Cartouche, proper right top acanthus spiral | 3 | 0.00 | 3.1 | 0.1 | 96.6 | 0.01 | 0.11 | 0.04 | 0.01 | 0.2 | 0.00 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Spigot, fleur-de-lys | 1 | 0.00 | 5.0 | 0.1 | 94.4 | 0.01 | 0.01 | 0.02 | 0.09 | 0.3 | 0.03 | 100.0 |  | Bruker Tracer III-SD |
| 82.DG.17 Lid, polished raised sheet | 3 | 0.00 | 5.1 | 0.0 | 95.0 | 0.01 | -0.03 | 0.00 | 0.01 | 0.1 | 0.01 | 100.2 |  | Bruker Tracer III-SD |
| 82.DG.17 Lion mask, nose | 3 | 0.00 | 3.5 | 0.1 | 96.2 | 0.00 | 0.11 | 0.00 | 0.01 | 0.1 | 0.00 | 100.0 |  | Bruker Tracer III-SD |
| 82.DG.17 Body, raised sheet, proper left | 3 | 0.00 | 2.6 | 0.0 | 97.0 | 0.00 | 0.03 | 0.01 | 0.07 | 0.3 | 0.02 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Handle, proper left | 3 | 0.00 | 3.2 | 0.2 | 96.1 | 0.00 | 0.03 | 0.00 | 0.11 | 0.4 | 0.02 | 100.0 |  | Bruker Tracer III-SD |
| 82.DG.17 Skirt, lower body, proper left maker's stamp | 3 | 0.00 | 2.0 | 0.0 | 97.9 | 0.02 | 0.05 | 0.02 | 0.02 | 0.1 | 0.00 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Putto, shoulder blade, proper left | 3 | 0.00 | 3.8 | 0.0 | 95.9 | 0.01 | 0.14 | 0.04 | 0.04 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Repair patch, upper acanthus | 3 | 0.00 | 3.9 | 0.1 | 96.0 | 0.00 | 0.01 | 0.00 | 0.01 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Base, front side, T-shaped geometric motif | 3 | 0.00 | 5.7 | 0.2 | 93.8 | 0.01 | 0.02 | 0.01 | 0.08 | 0.2 | 0.01 | 100.0 |  | Bruker Tracer III-SD |
| 82.DG.17 Rim of neck, gadroons | 4 | 0.00 | 3.1 | 0.0 | 96.5 | 0.01 | 0.08 | 0.02 | 0.08 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Flared foot, polished raised sheet | 4 | 0.00 | 5.5 | 0.1 | 93.9 | 0.00 | 0.10 | 0.01 | 0.08 | 0.3 | 0.03 | 100.0 |  | Bruker Tracer III-SD |
| 82.DG.17 Neck, burnished flute | 6 | 0.00 | 0.9 | 0.0 | 98.7 | 0.01 | 0.05 | 0.02 | 0.08 | 0.3 | 0.02 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Base, proper left, top surface | 4 | 0.00 | 5.5 | 0.0 | 94.0 | 0.02 | 0.09 | 0.02 | 0.08 | 0.3 | 0.01 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Cartouche, auricular mask | 5 | 0.00 | 1.9 | 0.0 | 97.8 | 0.01 | 0.13 | 0.03 | 0.01 | 0.2 | 0.00 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Repair patch, spot 2 | 3 | 0.00 | 4.3 | 0.0 | 95.8 | 0.00 | 0.00 | 0.01 | 0.01 | 0.1 | 0.01 | 100.2 |  | Bruker Tracer III-SD |
| 82.DG.17 Putto, proper left thigh | 3 | 0.00 | 4.4 | 0.1 | 95.3 | 0.00 | 0.08 | 0.02 | 0.04 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Body, raised sheet, proper right | 3 | 0.00 | 1.7 | 0.0 | 98.0 | 0.01 | -0.03 | 0.02 | 0.07 | 0.3 | 0.02 | 100.1 |  | Bruker Tracer III-SD |
| 82.DG.17 Waterfowl tap | 3 | 0.00 | 2.6 | 0.0 | 97.1 | 0.01 | 0.07 | 0.01 | 0.14 | 0.1 | 0.03 | 100.2 | **\*** | Bruker Tracer III-SD |
| 71.DG.76.1 Bowl, cartouche | 1 | 0.00 | 4.9 | 0.2 | 94.3 | 0.01 | 0.04 | 0.01 | 0.22 | 0.2 | 0.01 | 100.0 |  | Bruker Tracer 5i |
| 71.DG.76.1 Bowl, exterior | 3 | 0.00 | 2.8 | 0.0 | 97.1 | 0.00 | -0.02 | 0.01 | 0.14 | 0.1 | 0.00 | 100.1 |  | Bruker Tracer 5i |
| 71.DG.76.1 Bowl, handle | 2 | 0.01 | 2.8 | 0.0 | 96.8 | 0.01 | 0.07 | 0.01 | 0.19 | 0.1 | 0.00 | 100.1 |  | Bruker Tracer 5i |
| 71.DG.76.2 Basket, exterior, olive | 1 | 0.01 | 3.7 | 0.2 | 95.7 | 0.00 | 0.10 | 0.01 | 0.19 | 0.2 | 0.00 | 100.0 |  | Bruker Tracer 5i |
| 71.DG.76.3 Stand, bottom | 1 | 0.00 | 2.5 | 0.0 | 97.2 | 0.00 | 0.02 | 0.02 | 0.16 | 0.2 | 0.00 | 100.1 |  | Bruker Tracer 5i |
| 71.DG.76.3 Stand, bottom, wave | 1 | 0.00 | 1.6 | 0.0 | 98.1 | 0.01 | 0.02 | 0.01 | 0.17 | 0.1 | 0.00 | 100.1 |  | Bruker Tracer 5i |
| 71.DG.76.3 Stand, top | 1 | 0.00 | 3.0 | 0.1 | 96.6 | 0.01 | 0.04 | 0.01 | 0.16 | 0.2 | 0.00 | 100.1 |  | Bruker Tracer 5i |
| 71.DG.78 Bottom | 1 | 0.00 | 1.6 | 0.0 | 98.3 | 0.00 | -0.02 | 0.01 | 0.07 | 0.1 | 0.03 | 100.1 |  | Bruker Tracer 5i |
| 71.DG.78 Foot, bottom | 1 | 0.01 | 3.0 | 0.3 | 96.2 | -0.01 | 0.20 | 0.01 | 0.10 | 0.2 | 0.01 | 99.9 |  | Bruker Tracer 5i |
| 71.DG.78 Rim, bottom | 1 | 0.00 | 3.2 | 0.0 | 96.5 | -0.01 | 0.10 | 0.02 | 0.09 | 0.1 | 0.02 | 100.1 |  | Bruker Tracer 5i |
| 71.DG.78 Rim, top | 1 | 0.01 | 3.1 | 0.0 | 96.6 | 0.00 | 0.13 | 0.01 | 0.09 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 71.DG.78 Bottom, ball of solder(?) | 1 | 0.00 | 2.8 | 0.0 | 97.1 | 0.00 | -0.04 | 0.01 | 0.08 | 0.1 | 0.02 | 100.1 |  | Bruker Tracer 5i |
| 71.DG.78 Top, burnished | 1 | 0.00 | 3.9 | 0.0 | 95.9 | 0.00 | 0.08 | 0.01 | 0.08 | 0.1 | 0.03 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.12.1.b Tureen side, exterior (polished) | 1 | 0.00 | 3.0 | 0.1 | 96.0 | 0.00 | 0.08 | 0.01 | 0.13 | 0.6 | 0.00 | 99.9 |  | Bruker Tracer 5i |
| 82.DG.12.1.b Tureen interior, base | 1 | 0.00 | 2.0 | 0.0 | 97.7 | 0.00 | 0.07 | 0.01 | 0.15 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.12.1.b Tureen, coronet on armorial | 1 | 0.00 | 1.5 | 0.0 | 98.3 | -0.01 | 0.02 | 0.02 | 0.09 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.12.1.b Tureen, boar, snout | 1 | 0.00 | 3.7 | 0.0 | 96.0 | 0.01 | 0.15 | 0.01 | 0.09 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.12.1.b Tureen, armorial, polished lobe | 1 | 0.00 | 3.7 | 0.0 | 96.2 | 0.00 | -0.03 | 0.01 | 0.10 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.1.a Lid, cauliflower | 1 | 0.00 | 1.6 | 0.0 | 98.3 | 0.00 | -0.03 | 0.01 | 0.12 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.1.a Lid, crab pincer | 1 | 0.00 | 3.3 | 0.0 | 96.6 | -0.01 | 0.03 | 0.01 | 0.10 | 0.1 | 0.02 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.1.a Lid, interior | 1 | 0.00 | 0.6 | 0.0 | 99.2 | 0.00 | -0.05 | 0.01 | 0.16 | 0.1 | 0.00 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.1.a Lid, exterior | 1 | 0.00 | 3.3 | 0.1 | 96.2 | 0.01 | 0.12 | 0.02 | 0.15 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.1.b Liner, exterior bottom | 1 | 0.00 | 2.2 | 0.1 | 97.2 | 0.00 | 0.11 | 0.01 | 0.20 | 0.2 | 0.00 | 100.0 |  | Bruker Tracer 5i |
| 82.DG.13.1.b Liner, interior rim | 1 | 0.01 | 2.6 | 0.1 | 96.8 | 0.01 | 0.16 | 0.01 | 0.23 | 0.1 | 0.00 | 100.0 |  | Bruker Tracer 5i |
| 82.DG.13.1.c Tureen, exterior bottom and side | 2 | 0.00 | 2.9 | 0.1 | 96.7 | 0.01 | 0.07 | 0.01 | 0.16 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.1.c Tureen, interior rim | 1 | 0.00 | 1.6 | 0.0 | 98.0 | 0.02 | 0.08 | 0.01 | 0.17 | 0.2 | 0.01 | 100.0 |  | Bruker Tracer 5i |
| 82.DG.13.1.c Tureen, interior bottom | 1 | 0.01 | 0.2 | 0.0 | 99.3 | 0.01 | 0.13 | 0.01 | 0.20 | 0.1 | 0.00 | 100.0 |  | Bruker Tracer 5i |
| 82.DG.13.1.c Tureen, foot | 1 | 0.00 | 2.9 | 0.1 | 96.6 | 0.00 | 0.05 | 0.01 | 0.19 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.1.c Tureen, handle | 1 | 0.00 | 3.4 | 0.1 | 96.1 | 0.01 | 0.08 | 0.01 | 0.14 | 0.2 | 0.02 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.1.d Stand, back | 1 | 0.00 | 3.8 | 0.0 | 95.9 | 0.00 | 0.06 | 0.01 | 0.19 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.1.d Stand, front | 1 | 0.00 | 3.9 | 0.0 | 95.9 | 0.00 | 0.00 | 0.01 | 0.19 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.2.a Lid, cauliflower | 1 | 0.00 | 3.3 | 0.1 | 96.2 | 0.01 | 0.02 | 0.01 | 0.17 | 0.2 | 0.01 | 100.1 | **\*\*** | Bruker Tracer 5i |
| 82.DG.13.2.a Lid, crab pincer | 1 | 0.00 | 2.6 | 0.0 | 97.3 | -0.01 | 0.04 | 0.01 | 0.11 | 0.1 | 0.02 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.2.a Lid, interior | 1 | 0.00 | 0.5 | 0.0 | 99.2 | 0.00 | -0.04 | 0.01 | 0.20 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.2.a Lid, exterior | 1 | 0.00 | 3.3 | 0.1 | 96.2 | 0.01 | 0.02 | 0.01 | 0.17 | 0.2 | 0.01 | 100.1 | **\*\*** | Bruker Tracer 5i |
| 82.DG.13.2.b Liner, exterior bottom | 1 | 0.00 | 3.1 | 0.1 | 96.5 | 0.01 | 0.00 | 0.01 | 0.17 | 0.2 | 0.00 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.2.b Liner, interior rim | 1 | 0.00 | 3.4 | 0.0 | 96.2 | -0.01 | 0.03 | 0.01 | 0.18 | 0.2 | 0.00 | 100.1 | **\*** | Bruker Tracer 5i |
| 82.DG.13.2.c Tureen, exterior bottom (polished) | 1 | 0.00 | 2.5 | 0.0 | 97.3 | 0.00 | 0.08 | 0.01 | 0.04 | 0.1 | 0.02 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.2.c Tureen, exterior side | 1 | 0.00 | 4.4 | 0.0 | 95.5 | 0.00 | 0.03 | 0.01 | 0.05 | 0.1 | 0.02 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.2.c Tureen, interior rim | 1 | 0.00 | 0.9 | 0.0 | 99.0 | 0.00 | 0.01 | 0.01 | 0.06 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.2.c Tureen, interior bottom | 1 | 0.00 | 0.5 | 0.0 | 99.4 | 0.01 | 0.04 | 0.02 | 0.06 | 0.1 | 0.01 | 100.0 |  | Bruker Tracer 5i |
| 82.DG.13.2.c Tureen, foot | 1 | 0.00 | 2.0 | 0.0 | 97.7 | 0.00 | 0.09 | 0.01 | 0.19 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.2.c Tureen, handle | 1 | 0.00 | 3.8 | 0.1 | 95.7 | 0.00 | 0.11 | 0.01 | 0.17 | 0.2 | 0.02 | 100.1 |  | Bruker Tracer 5i |
| 82.DG.13.2.d Stand, back | 1 | 0.00 | 4.0 | 0.0 | 95.8 | -0.01 | 0.04 | 0.01 | 0.20 | 0.2 | 0.01 | 100.2 |  | Bruker Tracer 5i |
| 82.DG.13.2.d Stand, front | 1 | 0.00 | 3.3 | 0.0 | 96.6 | 0.01 | -0.04 | 0.01 | 0.19 | 0.1 | 0.01 | 100.2 |  | Bruker Tracer 5i |
| 84.DG.744.1.a Lid, basket | 1 | 0.00 | 1.1 | 0.1 | 98.4 | 0.00 | -0.03 | 0.01 | 0.29 | 0.2 | 0.00 | 100.0 |  | Bruker Tracer 5i |
| 84.DG.744.1.a Lid, flower | 1 | 0.01 | 1.3 | 0.0 | 98.4 | -0.01 | -0.02 | 0.02 | 0.24 | 0.2 | 0.00 | 100.1 | **\*\*** | Bruker Tracer 5i |
| 84.DG.744.1.b Vessel, exterior | 1 | 0.00 | 2.4 | 0.0 | 96.9 | 0.01 | 0.12 | 0.01 | 0.22 | 0.4 | 0.02 | 100.0 |  | Bruker Tracer 5i |
| 84.DG.744.1.b Vessel, exterior base, side | 1 | 0.01 | 1.7 | 0.0 | 97.6 | -0.01 | -0.03 | 0.01 | 0.24 | 0.5 | 0.00 | 100.0 |  | Bruker Tracer 5i |
| 84.DG.744.1.b Vessel, flower | 1 | 0.00 | 1.0 | 0.0 | 98.7 | -0.01 | -0.01 | 0.01 | 0.24 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 84.DG.744.1.b Vessel, exterior textured surface | 1 | 0.00 | 3.6 | 0.0 | 96.0 | -0.01 | 0.03 | 0.01 | 0.19 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 84.DG.744.2.a Lid, basket | 1 | 0.00 | 1.3 | 0.0 | 98.3 | 0.01 | 0.08 | 0.01 | 0.25 | 0.1 | 0.00 | 100.1 |  | Bruker Tracer 5i |
| 84.DG.744.2.a Lid, flower | 1 | 0.01 | 1.1 | 0.0 | 98.5 | 0.01 | 0.08 | 0.01 | 0.27 | 0.1 | 0.00 | 100.1 | **\*\*** | Bruker Tracer 5i |
| 84.DG.744.2.b Vessel, exterior | 1 | 0.00 | 1.3 | 0.2 | 97.9 | 0.00 | 0.03 | 0.01 | 0.21 | 0.3 | 0.01 | 99.9 |  | Bruker Tracer 5i |
| 84.DG.744.2.b Vessel, exterior base, side | 1 | 0.00 | 3.1 | 0.0 | 96.2 | -0.01 | 0.07 | 0.01 | 0.28 | 0.3 | 0.00 | 100.1 |  | Bruker Tracer 5i |
| 84.DG.744.2.b Vessel, flower | 2 | 0.00 | 1.3 | 0.0 | 98.2 | 0.00 | 0.07 | 0.01 | 0.18 | 0.2 | 0.01 | 100.0 |  | Bruker Tracer 5i |
| 2005.43 Rabbit | 1 | 0.00 | 2.6 | 0.0 | 97.1 | 0.01 | 0.09 | 0.01 | 0.17 | 0.1 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 2005.43 Cauliflower | 1 | 0.02 | 1.3 | 0.0 | 98.3 | 0.00 | 0.18 | 0.01 | 0.14 | 0.1 | 0.00 | 100.1 | **\*\*** | Bruker Tracer 5i |
| 2005.43 Base, front | 1 | 0.00 | 3.7 | 0.0 | 96.0 | 0.00 | 0.03 | 0.02 | 0.14 | 0.2 | 0.02 | 100.1 |  | Bruker Tracer 5i |
| 2005.43 Ground (repoussé) | 1 | 0.00 | 1.3 | 0.0 | 98.3 | 0.01 | 0.04 | 0.01 | 0.18 | 0.2 | 0.01 | 100.1 |  | Bruker Tracer 5i |
| 2005.43 Rim, inside | 1 | 0.00 | 3.1 | 0.1 | 96.6 | 0.00 | 0.01 | 0.02 | 0.12 | 0.1 | 0.03 | 100.1 |  | Bruker Tracer 5i |
| 2005.43 Snipe, proper right leg | 1 | 0.03 | 2.3 | 0.0 | 97.3 | 0.00 | 0.11 | 0.01 | 0.16 | 0.1 | 0.00 | 100.1 | **\*\*** | Bruker Tracer 5i |
| 2005.43 Solder pallion, underside | 1 | 0.00 | 1.5 | 0.3 | 98.1 | 0.00 | 0.00 | 0.01 | 0.04 | 0.1 | 0.01 | 99.9 |  | Bruker Tracer 5i |
| 84.DG.42.2 Putti thigh | 1 | 0.00 | 2.4 | 0.0 | 97.2 | 0.00 | 0.03 | 0.02 | 0.13 | 0.1 | 0.01 | 100.0 |  | Bruker Artax |
| 84.DG.42.2 Putti back | 1 | 0.00 | 4.1 | 0.1 | 95.6 | 0.00 | 0.05 | 0.02 | 0.09 | 0.2 | 0.02 | 100.1 | **\*** | Bruker Artax |
| 84.DG.42.1 Putti thigh | 1 | 0.00 | 3.7 | 0.0 | 96.0 | 0.01 | 0.08 | 0.02 | 0.08 | 0.1 | 0.01 | 100.1 |  | Bruker Artax |
| 84.DG.42.1 Putti back | 1 | 0.00 | 4.4 | 0.1 | 95.3 | 0.00 | 0.01 | 0.02 | 0.09 | 0.2 | 0.02 | 100.0 |  | Bruker Artax |
| 88.DH.127.2 Vessel, exterior tie wrap | 1 | 0.01 | 3.9 | 0.0 | 95.7 | 0.01 | 0.05 | 0.01 | 0.11 | 0.3 | 0.03 | 100.0 |  | Bruker Artax |
| 88.DH.127.2 Vessel, catch-latch rim | 1 | 0.00 | 1.1 | 0.1 | 98.4 | 0.01 | 0.09 | 0.01 | 0.28 | 0.1 | 0.01 | 100.1 |  | Bruker Artax |
| 88.DH.127.2 Vessel, ring attached to rim | 1 | 0.00 | 1.0 | 0.1 | 98.6 | 0.02 | 0.37 | 0.04 | 0.29 | 0.2 | 0.01 | 100.5 |  | Bruker Artax |
| 88.DH.127.2 Vessel, exterior bottom | 1 | 0.00 | 0.7 | 0.0 | 99.0 | 0.00 | 0.02 | 0.01 | 0.15 | 0.1 | 0.01 | 100.0 |  | Bruker Artax |
| 88.DH.127.2 Vessel, threaded rod bottom | 1 | 0.00 | 1.8 | 0.1 | 97.6 | 0.01 | 0.11 | 0.02 | 0.26 | 0.2 | 0.01 | 100.1 |  | Bruker Artax |
| 88.DH.127.2 Lid, flower petal | 1 | 0.00 | 1.0 | 0.0 | 98.7 | 0.01 | 0.08 | 0.01 | 0.11 | 0.2 | 0.02 | 100.1 |  | Bruker Artax |
| 88.DH.127.2 Lid, catch-latch rim | 1 | 0.00 | 1.1 | 0.1 | 98.3 | 0.00 | 0.11 | 0.02 | 0.26 | 0.2 | 0.01 | 100.1 |  | Bruker Artax |
| 88.DH.127.2 Lid, exterior side | 1 | 0.00 | 3.8 | 0.0 | 95.7 | 0.01 | 0.01 | 0.01 | 0.12 | 0.3 | 0.03 | 100.0 |  | Bruker Artax |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Errors (95% C.I.4) |  | 0.01 | 0.7 | 0.1 | 2.3 | 0.08 | 0.04 | 0.03 | 0.02 | 0.2 | 0.02 |  |  | Bruker Tracer 5i |
|  |  | 0.01 | 0.6 | 0.2 | 1.7 | 0.04 | 0.05 | 0.03 | 0.03 | 0.2 | 0.03 |  |  | Bruker Artax |
|  |  | 0.02 | 0.6 | 0.1 | 1.7 | 0.08 | 0.04 | 0.04 | 0.02 | 0.2 | 0.03 |  |  | Bruker Tracer III-SD |

\* Silver L/K ratio elevated.

\*\* Silver L/K ratio depressed.

1 Values in gray are below the detection limit (defined as “critical value” at 95-percent confidence per {{Kadachi et al. 2012}}).

2 Number of measurements taken at each site.

3 Quantitative results have not been normalized; totals do not always add up to exactly 100 percent.

4 A 95-percent confidence interval represents the range above and below the estimated value within which the true value is likely to fall, with a confidence of 95 percent. See additional discussion above.