Appendix: Table 2

XRF results for gilded surfaces, showing the amount of mercury remaining in the gold

|  |  |  |  |
| --- | --- | --- | --- |
| Sample | **Au-L** | **Hg-L** | Estimated wt.% Hg in Au |
| 71.DG.77.a Lid, exterior | 14.5 | 0.18 | 1.2 |
| 71.DG.77.a Lid, interior | 13.3 | 0.85 | 6.4 |
| 71.DG.77.b Bowl, interior | 18.4 | 1.03 | 5.6 |
| 71.DG.77.b Bowl, exterior | 17.4 | 0.26 | 1.5 |
| 71.DG.77.b Handle, proper right underside | 22.5 | 0.55 | 2.5 |
| 71.DG.77.b Handle, proper left underside | 22.1 | 0.55 | 2.5 |
| 71.DG.76.1 Sauceboat, interior | 34.1 | 0.87 | 2.5 |